Battery Degradation Modeling, Anomaly Detection, and Remaining Useful Life Estimation

1. Methodology

This study presents an complete analytical study for lithium-ion cells degradation analysis, anomaly detection, and remaining useful life (RUL) estimation using laboratory cycling data. The methodology integrates physics-based modeling, statistical analysis, and machine learning techniques.

1.1 Data Processing

Raw lab cycling data

The dataset consists of laboratory cycling measurements collected from lithium-ion cells under controlled charge–discharge protocols. The raw data includes time-series signals such as voltage, current, capacity, and cycle index. These measurements provide operating conditions and provide insight into electrochemical aging behavior.

Feature extraction

From the per-cycle data, the following features were extracted. The since initial capacity was not given it was assumed with dummy number. This can be changed upon getting the original value. As this parameter is changable:

- Discharge capacity (Ah) as the primary degradation indicator

- Coulombic efficiency (CE), defined as the ratio of discharge to charge capacity

- Energy throughput (charge and discharge energy per cycle)

These features form the basis for degradation modeling, anomaly detection, and RUL prediction.

1.2 Degradation Modeling

n capacity fade model

Capacity degradation was modeled using a square-root-of-cycle-count (n) formulation:

Qn= Q0,fit-an

This model is physically used by diffusion-limited processes such as solid–electrolyte interphase (SEI) growth and has been widely reported to capture long-term aging behavior under cycling conditions.

Parameter estimation

Model parameters were estimated using regression techniques on a subset of clean cycles. By fitting the model only to representative, non-anomalous cycles, the fitted parameters reflect the true degradation trend rather than being biased by noise or outliers.

1.3 Anomaly Detection

Residual-based features

For each cycle, residuals were calculated as the difference between measured capacity and model-predicted capacity. These residuals isolate deviations from the expected degradation trend and serve as physics-aware anomaly identifiers. Residuals were normalized using z-scores to account for cell-to-cell variations.

DBSCAN clustering

Unsupervised anomaly detection was performed using DBSCAN (Density-Based Spatial Clustering of Applications with Noise). Feature vectors composed of ΔQ, discharge capacity, and coulombic efficiency were standardized and clustered. Cycles classified as noise (cluster label = −1) were flagged as anomalous.

Motivation for unsupervised learning

Unsupervised methods were chosen because labeled anomaly data is typically unavailable in battery aging experiments. DBSCAN enables detection of abnormal cycles without prior assumptions about anomaly frequency or distribution, making it well suited for exploratory and production-scale analytics.

1.4 Remaining Useful Life (RUL) Prediction

RUL estimation was implemented via √n capacity extrapolation. For each cell, model parameters were estimated from cycle-level data, with an optional mid-life fitting mode (use_mid_life=True) that excludes very early cycles (Cycle < 5) to reduce formation-related bias.

End-of-life (EOL) was defined as the cycle at which discharge capacity reaches 80% of the measured initial capacity:

- Q0,meas= max⁡(Q)

- QEOL= 0.8* Q0,meas

- Solving the fitted model for the EOL cycle count:

ηEOL= Q0,fit- QEOLa2

RUL at a given operating point ηnow​ is then:

RULηnow= ηEOL- ηnow

This provides an interpretable baseline RUL estimator suitable for benchmarking more complex methods.

2. Key Findings

- The n degradation model captures the dominant long-term capacity fade trend accurately across both cells.

- Early-life RUL prediction (<30% of lifetime) is inherently unreliable due to limited degradation signal and high uncertainty.

- Incorporating mid-life data significantly improves EOL and RUL prediction accuracy, as degradation trends become more stable.

- Residual-based anomaly detection successfully identifies cycles with abnormal efficiency loss or sudden capacity deviations.

- DBSCAN clustering isolates anomalous cycles without requiring labeled data, improving robustness of downstream modeling.

- LSTM-based sequence modeling is architecturally appropriate for RUL prediction but is constrained by data volume and diversity in this study.

- Among the two cells, Cell 01 is the weakest one.

3. Limitations

Several limitations should be acknowledged to contextualize the results:

- The analysis is based on a limited number of laboratory-tested cells, restricting generalization.

- Temperature data and thermal gradients were not available due to no data of temperatures, despite their strong influence on degradation.

- Cell balancing and pack-level interactions were not explicitly modeled.

These limitations highlight areas for future improvement.

4. Extensions to Fleet Analytics and Battery Passport Reporting

4.1 Fleet analytics

The proposed framework naturally extends to fleet-scale analytics by aggregating per-vehicle degradation indicators and RUL estimates. Fleet-level analysis enables:

- Identification of fast-aging vehicles

- Prioritization of predictive maintenance actions

- Warranty planning

Early anomaly detection at the vehicle level can prevent dangerous failures and optimize fleet utilization.

4.2 Battery passport relevance

The extracted metrics align closely with emerging EU Battery Passport requirements. Specifically:

- The battery passport is kind of digital certificate which includes both statistic parameters and dynamic parameters.

- The static parameters are BOL capacity, Nominal voltage, Initial range as per specs etc.

- The dynamic parameters are State-of-health (SoH) and RUL indicators for transparency, number of high temperature events, high soc charging events etc.

5. Conclusion

This work presents a comprehensive, end-to-end pipeline for battery degradation modeling, anomaly detection, and RUL estimation. Physics-based, statistical, and machine learning approaches were systematically compared, highlighting their respective strengths and limitations. From the above analysis the Cell-01 is weakest cell among the two cells.